## Slide 1: Grid Chat

## Slide 2
Twist Boundary
Tilt Boundary
Diffraction
Conditions
D= 3 nm
Relaxation
Time
D= 3 nm
Relaxation
Time
D= 1 nm
Notes: Twist boundaries have same behavior as tilt boundaries. But, the magnitude of their scattering potential is smaller.
Observed turnover even without rotation term
Get turn over with or without rotation??

## Slide 3
Twist Boundary: m=0 conditions
Tilt Boundary:
is 0 for the m=0 condition. Therefore, the only non-zero term comes from rotation, and without rotation the relaxation time would diverge
Twist Boundary:
N-array:
(b in z, spaced in y)
M-array:
(b in y, spaced in z)
is 0 for the m=0 condition. Only one strain component goes to 0.
is 0 for the m=0 condition. Only one strain component goes to 0.
Notes: Twist boundaries have same behavior as tilt boundaries. But, the magnitude of their scattering potential is smaller.
PLOT the strain fields!!
Get turn over with or without rotation??

## Slide 4: Heterointerfaces Boundaries
Strain relaxation also often occurs through twinning (60° mixed)
Elastic Energy (per unit area) due to strain at the epilayer from two perpendicular periodic dislocation arrays:
  Homogeneous strain: Related to lattice mismatch and misfit dislocation burgers vector
  Fluctuating elastic field (per unit length of the dislocation line): due to the fluctuating elastic field
  Good model of residual strain at the “core”?
  In the literature, people don’t describe the long range strain fields
  Measured strain fields from HRTEM: https://www.nature.com/articles/nmat1057.pdf?proof=true

## Slide 5: Van der Merwe Strain fields
Notes: Treating a single array. “Plane strain” problem.
What’s up with the colorbars?

## Slide 6: Twins Schematic